How to print with T-Glase (PETT)

T-glase is a blend of high strength PETT released by Taulman 3D. It’s a clear flexible material, neatly identical to the material that plastic bottles are usually made of. The PETT doesn’t degrade at extrusion temperature, so it’s a great material for those looking to melt and reuse their scrap (you can even blend in used soda bottles for up to 12% of the mixture).

You can read a lot more about this at their website, including a great writeup on using the material to print short ‘light tubes’ that can redirect light in printed applications.

Pros:
- Extrudes well @ 212C -230C and bonds well to itself
- Optically clear, though the uneven surfaces of a printed part will still scatter light
- Can be recycled into new filament
- High strength material
- FDA approved for food contact
Cons:
- High strength parts tend to require high infill
- Has a lower glass transition temperature than ABS, so parts will soften a bit at temperatures around 78C
- More expensive that standard printing materials (~2X ABS/PLA cost)
- Must be printed much more slowly than most materials, with a maximum printing speed of about 30mm/s
- Overhangs tend to curl upwards without a fan on the nozzle

Nozzle Temperature:	200-230 C (212 default)
Bed Temperature:	0-70 C (60 default)
Nozzle sizes:	.35-.1.5mm
Print speed:	15-30 mm/s

Printing Tips:
T-Glase will print on about any surface; acrylic, glass, painters tape or the PET covered glass that we normally use with the TAZ and AO series printers. It tends to stick to the nozzle and will start to tear at speeds above 30mm/s with the temperature set to 225C. You can increase the temperature to allow higher printing speeds, but part finish is better at temperatures between 210 and 230 C. T-glase prints best at very high, almost solid infill settings (80-100%), though it will print honeycomb infill down to 7.5%.

Sample Configuration:
; layer_height = 0.25
; perimeters = 3
; top_solid_layers = 5
; bottom_solid_layers = 2
; fill_density = 0.95
; perimeter_speed = 25
; infill_speed = 25
; travel_speed = 100
; nozzle_diameter = 0.5
; filament_diameter = 2.89
; extrusion_multiplier = 1
; perimeters extrusion width = 0.42mm
; infill extrusion width = 0.55mm