  CURA Profile Creation and Revision Process

Using either, the completed New Material Testing Report OR sample models of prints using the current profile associated with the filament, make a Slice Plan indicating the needed improvements and the estimated changes to fix them.

SLICE PLAN TEMPLATE (please save in appropriate filament folder with other testing documents)
Filament Type:
General Assessment:
Cosmetic Notes:
Structural Notes:
Other Notes:
Slice Setting Expectations:

PLEASE REMEMBER TO FILL OUT YOUR Printing Log AFTER EVERY FINISHED AND FAILED PRINT!!

TESTING PROCEDURE

Begin with model #1, making edits and notes for every failed print and setting change in your personal Printer Log. When you are satisfied with the quality of model #1, move on to printing model #2 to confirm. If model #2 passes, move on to model #3. If model #2 is unsatisfactory, make SMALL setting revisions to improve. When you feel that model #2 is correct, take the newly edited profile and reprint model #1 with it to verify. If you find yourself making significant edits to the profile many models into the process, you MUST go back and reprint the previous test models with the new profile to verify it is still satisfactory for those models.

HELPFUL DATA TIP! When making setting edits after the start of the process, print a model after each change. DO NOT make multiple changes in between testing models, you will not be able to know which change is effecting your profile results.

TESTING STEPS
(recommended models found here: /home/aleph/shared-j/Documents/R&D/material-testing/toolbox/test-stls/basic testing stls/)
(*what are we looking for?)

1) Average Model (recommended model: benchy)
*Varied Shape and Size - This test requires a variety of geometric shapes AND sizes,making it a
helpful place to start.

2) Bridging Test (recommended model: bridging) (*bridging)
*Bridging - This will test its bridging and help you find the appropriate printing temps and fan
settings.
(tip: this is also a good model to help find out if your filament is wet, water=stringing,	bad bridging and weak layer adhesion)

3) Fine Detail (recommended model: spikes)
*Fine Detail, Stringing, Retraction - This test will make sure your retraction settings and fine
details print appropriately.

4) Full Build Volume Infill (recommended model: flat-square) (increase model size to full build plate size)
*Full Build Volume - This test is to ensure that the fan and print temp are balanced enough to
print the full print volume area that is capable by the machine.

5) Delicate Design Model (recommended model: spiral)
*Stringing, Thin Structure Accuracy and Overhang - This test doesn’t need to be small, it just	needs to have a thinner, taller build so you can verify that the print will remain on the bed and	not warp up on thinner overhang areas.

6) Fit/Swell/Shrink (recommended model: negative space)
*Workability, Geometric Accuracy - This test is to assess how much this material swells or
shrinks during printing and how it will fit into itself if used to print a complex part.
EXTRA! - for further fit testing you can also use the gears.stl to test workability when
printed together and bolt.stl and screw.stl when printed separate.

7) Support (recommended model: for high detail – elf-bust.stl; for low detail – bunny.stl)
*Support - This test is to set support settings. (NOTE: you do not need to reprint previous
models for support setting changes)

8) Spiral vase (recommended model: splatbag.stl)
*Spiralize - This test is to test the spiralize outer contour setting.

9) Retraction Torture Test (recommended model: eiffel-tower.stl)
*Strip Out Test - OPTIONAL: Use this if there is a concern for material strip-outs or errors in
high detail accuracy.

You have completed the Profile Testing Process. Submit your completed profile on Code.alephobjects.com and wait for feedback from larger group testing and refer to the Profile Feedback Checklist for details on those ticket errors.