LulzBot Filament Testing Report

Manufacturer:	Colorfabb
Filament Name:	N-GEN
Filament Type:	Amphora 3300
Tested By:	Brent M
Date:	12/26/2015

Ease of use:	8/10
Appearance:	9/10
Size consistency:	10/10
Color consistency:	10/10
Print temperature:	230/75
Prints using Lulzbot profiles/temps: Yes, profiles had to be created for this material

Notes:
- ~70C glass transition temperatures
- Top surfaces and bridging are great, much better than 1800.
- Filament size and color consistency are great.
- The unlabeled spools make it VERY easy to mix up with other Colorfabb materials

Recommendation: This material prints reasonably well over a wide range of temperatures, making it a very forgiving material for new users or complex prints. Surface finish quality and interlayer adhesion are great, and prints are strong and flexible. Print speeds can be set fairly high (similar to PLA speeds). This material is definitely approved and should be a strong contender with ABS or PLA as a general purpose printing material.

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
Colorfabb N-GEN (2.85mm)	XXX-XXXmm in 10m sample / (<2%)	XXX-XXXmm (0.04mm)	230/75 worked well