LulzBot Filament Testing Report

Manufacturer: ColorFabb
Filament Type: nGen Flex
Tested By:	bam
Date:	02.06.17

Ease of use:	5/10
Appearance:	10/10
Color consistency:	10/10
Print temperature Range (C):	250-260/90-110

Variance in diameter: (2.82-2.84mm)
Minimum bend radius: NA, can tie in knot
Prints using current Lulzbot profiles/temps: No, prints well with modified PLA profiles (see notes)

General Notes:
- Unfortunately, this material does not stick well to PEI, gluestick or straight glass.
  - Small parts >50mm to a side will likely print reasonably well with a brim
  - larger parts than this lift even with a brim
- This material has the same shiny appearance as nGen
- Wiping and probing at 160C works well.
- It prints well with a standard extruder at similar speeds to PLA, but can and will buckle in the filament path if pushed too fast or if the first layer is over squished
- Seems to do well without fan
- The material warps moderately, would likely print well if a good solution for bed adhesion is found.
- Same hardness (95A) as Ninjatek Semiflex, similar to PCTPE
- It sounds like hairspray and high head may work, have not been able to verify.
Health or environmental risks:

Inhalation: None known.
Ingestion: None known.
Skin contact: Molten material will produce thermal burns.
Eye contact: Molten material will produce thermal burns.

This product does not contain any carcinogens or potential carcinogens as listed by OSHA, IARC or NTP.

Disposal Options:

Disposal methods: Dispose of waste and residues in accordance with local authority
requirements. Incinerate.

Recommendation:
While it’s awesome that nGen flex prints so well through a standard extruder, the difficulty involved in getting parts to stick to any current bed surface hurts its usefulness for most applications. If a bed adhesion solution is found this material should be revisited as an alternative to PCTPE / semiflex.