Enye labs Filament testing notes:

Manufacturer:	Enye labs
Filament Name:	Recycled PET Batch 2– Natural – 3mm
Recycled PET Batch 2– Red – 3mm
Filament Type:	PET – 100% recycled
Date:	9/8/2015

Ease of use:	2/10
Appearance:	Good color – looks like what you'd expect from soda bottles
Size consistency:	Poor – Out of round from ~2.8mm to 2.4mm
Color consistency:	Good, some black contaminants
Print temperature:	240/60 (LulzBot Mini)
Prints using Lulzbot profiles/temps: No

Notes:
b-pet - Red
- Filament size consistency was extremely poor on the red dyed filament, being out of round from 2.85mm maximum in the major dimension to 2.24mm minimum in the minor dimension. This causes the filament to strip much more readily if loaded into the toolhead with the narrow side pressed into the hobbed bolt.
- This filament has a very narrow print temperature range between being able to extrude at all (~240) to where it starts to boil (245). At 245C there were huge inconsistencies in the pressure required to feed. Feeding filament manually by hand at 245C, it's very clear that there are sections that melt more readily than others, resulting in the necessity to print the filament above the temperature that it starts boiling at in order to prevent filament stripping.
- The filament boiled badly at just over the minimum extrusion temperature, similar to nylon filaments that have absorbed water. This leads to inconsistent printing and poor surface finish. It might be dealt with with a better drying process of the filament prior to being extruded into filament.

Recommendation:

This filament is a great concept, but not quite there yet. It is more finicky to print with than t-glase, but with a lower pricepoint and 100% recycled content I think a lot of people would prefer it if we could print consistently with it. For this to happen, the

Filament diameter accuracy / consistency:

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
B-PET (red 3mm batch 2 / )	2.24mm – 2.88mm	2.42-2.84mm