LulzBot Filament Testing Report

Manufacturer:	Esun
Filament Name:	Conductive
Filament Type:	Conductive Nylon
Tested By:	Patrick
Date:	5/8/2015

Ease of use:	Extremely difficult
Appearance:	Black
Size consistency:	Average
Color consistency:	Good
Print temperature:	220-260
Prints using Lulzbot profiles/temps: Had to make new conductive profile

Recommendation: I would not recommend we sell this filament. It is extremely difficult to print with. Prints suffer from delamination between layers and warping. After the filament is heated it becomes extremely brittle most parts broke just trying to take them off the bed. Tried all the temperatures between 220-260C having different issues at various temperatures. All the reels had visible bubbles in the in the filament even the one that was just removed from a vaccume sealed bag. You can hear a hissing/popping noise from bubbles as the filament is extruded.

Notes:
- Water or gas in filament.
- Filament Bubbles above 230C and does not adhear to itself at 230C and below.
- Warping/Delamination/Bed adhesion problems.
- Least conductive material we have tested so far.
- Brittle parts.
- 20% of filament is material called carbon black which is being evaluated as a possible carinogenic to humans by the IARC. (not sure if this crediable but might be worrisome)
- Carbon Black material took over 1000mm of filament to purge when changing filament.
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
Conductive Nylon	2.86-2.97 (.11mm)	.6mm (2.91-2.97)	220-260(Found best temp to be between 240-250C)

Illustration 1: Bubbles in filament on reel