Esun Filament testing notes 2:

Notes:
PETG Yellow 1.75mm
- Stuck to glass bed very well without any adhesive.
- Not the best material for bridging.
- This material is super strong.
PLA Silver 3mm
- Prints well we have had trouble with silver colored filaments before.
- Silver parts have a glossy look to them.
ABS Blue 3mm
I didn't use the best settings when printing this but it prints like any other abs.
Laywood Brown 1.75mm
- It looks more like PLA than laywood compared to others like it.
- The color is cool unique one.
- Had to turn the bed temp up to 80 to get it to stick.
  Laywood Nature 1.75mm
- Prints similar to the brown is extremely brittle, filament broke while feeding into filament guide.
- Looks like tan PLA but it breaks easier and doesn't stick as well.
  Nylon 1.75mm
- Is difficult to print with like most nylon.
- Used a lot of glue stick to get it to stick on the bed.
  HIPPS Green 1.75mm
- It prints awesome just like every HIPPS filament.
  Flexible 1.75mm
- Has the consistency of bubblegum.
- Could not get it to print filament bends when feeding.
- We could maybe print this if we ever made a flexystruder that was 1.75mm.
  UV to Red 1.75mm
- Has the consistency of bubblegum.
Recommendation: .

Filament diameter accuracy / consistency:

Filament	Variance in diameter	Maximum round	Extrusion temperature
PETG	1.67-1.73 (.6mm)	0.01mm (1.72-1.73)	230-250C (printed at 240C with .5mm hex nozzle, bed temp 100C)
PLA Silver	2.79-2.91 (.11mm)	0.01mm (2.9-2.91)	190-220C (printed at 190C with .5mm hex nozzle)
ABS Blue	2.84-2.91 (.6mm)	0.03mm (2.88-2.91)	220-230C (printed at 230C with .5mm hex nozzle)
Laywood Brown	1.58-1.66 (.5mm)	0.06mm (1.60-1.66)	190-200C (printed at 190C with .5mm hex nozzle)
Laywood Nature	1.63-1.72 (.9mm)	0.03mm / (1.69-1.72)	190-200C (printed at 190C with .5mm hex nozzle)
Nylon	1.70-1.78 (.8mm)	0.03mm / (1.75-1.78)	230-260C(printed at 250 with .5mm hex nozzle)
HIPPS Green	1.61-1.73 (.12mm)	0.02mm / (1.71-1.73)	220-230C(printed at 230 with .5mm hex nozzle)
Flexible	1.62-1.68 (.6mm)	0.01mm / (1.67-1.68)	190-220C(printed at 200 with .5mm hex nozzle)
UV to Red	1.75-1.77 (.3mm)	.01 mm / (1.76-1.77)
Average	1.75mm (+/- .45mm)	0.025mm