LulzBot Filament Testing Report

Manufacturer: Esun
Filament Type: PVA
Tested By: Ben B.
Date: 9/8/2017

Ease of use:	10/10
Appearance:	10/10
Color consistency:	N/A
Print temperature Range (C): 190c-220c
Variance in diameter: 2.85mm – 2.89mm
Minimum bend radius:
Prints using current Lulzbot profiles/temps: Esun PVA

General Notes:	(Be as detailed as possible)
- Gluestick helps initial plate adhesion
- Adheres well to most filaments
- Runs well with most filament around the same extrusion temperature
- Dissolves quickly and comes off parts well.

Recommended Print Profiles: PLA at 195C

Health or environmental risks: Do not print above 240c

Disposal Options: Contact local waste authorities

Recommendation:

This is the best dissolvable support I’ve used so far, especially for PLA support material. Use interface layer in Cura2 for even better adhesion to PLA part. Create a nice looking finish were support was when removed. This PVA dissolves quickly, you can have a cleaned part much faster than other support materials. The PVA starts to fall off within minutes of immersion in water.

Revision History

Revision Date	Modifications or Additions	Updated By