LulzBot Filament Testing Report

Manufacturer: IC3D
Filament Type: PETG 6763
Tested By: Angelica Suiter
Date: 11/29/2017 (start)

NOTE: ONLY CLEAR MATERIAL HAS BEEN TESTED AT THIS TIME, COLOR ASSESSMENTS AND PROFILES MAY VARY

Ease of use: 10/10
Appearance: 10/10
Color consistency: Clear batch – Consistent clarity 10/10
Print Temperature Range (C): 215-250 C (230 C Recommended)
Variance in diameter:
Minimum bend radius: 25 mm bend radius before a fold appears
Current Lulzbot profiles/temps Used for Tests:
I had already been testing PETG profiles for other suppliers and used those to test, they were based off of the nGen profiles with minor adjustments
General Notes:
- Thermal Decomp: “Thermal stability not tested, low stability hazard expected at normal operating temps” (check SDS) – This doesn’t concern me too much, the auto ignition temp is the same as other PETG (autoignition temp: 454 C)
- Packaging: test reels only delivered (revision, box with colored logo and an open viewing window to see the material, inside reel sealed with moisture absorbing packet inside bag)
- Diameter variance:
- Consistent clarity and texture, no debris found.
- Temp range for extrusion: 180-290 C – (Recommend print temp range: 215-250 C)
- Extruded at 290 C, no bubbling or bad small or result, just a thinner extrusion.
- Oozes at 235-240 C
- Bed temp: Sticks at 60 C, 65-75 C recommended.
- No snap point on bend test, 25mm radius bend before deformation
- Does not break along layer lines, when broken, it will follow its material as if injection molded. I have noticed that if a part is already damaged it will be easier for the compromised area to allow for breaks (example is opening a plastic food package with your teeth, you make a small cut and allow the tear to follow through the material)
- thinner lower layers are more brittle upon rare occasion, this is consistent with PETG results of other suppliers. ***PETG does not heat, cool and reheat well, the heating and cooling of the nozzle for probing and temping up compromises the filament sitting in the toolhead, slicing parts with greatly expanded skirts can help purge the compromised material and help ensure the strength of the part.
Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)
- High Speed - Recommended
- Standard - Recommended
- High detail – Undetermined, thinner layers cause issue when bridging (0.2mm and less)
Health or environmental risks:
- Do not Eat
- Do not touch molten material
- Nothing New, Not classified as a hazardous material, nor are any of its components.
Disposal Options:
Dispose of contents/container to an appropriate treatment and disposal facility in accordance with applicable laws and regulations, and product characteristics at a time of disposal.
Recommendation:
- Recommended
- Prints well for a clear material, I would like to further test colors and compare.
- Brittle lower layers found rarely, ***refer to skirt purge fix.
Revision History

Revision Date	Modifications or Additions	Updated By
11/29/17	BEGAN TESTING	A. Suiter
01/11/2018	Paperwork Update	A. Suiter
1/25/2018	Packaging notes	A. Suiter