Lulzbot Filament Testing Report
Manufacturer: Polymaker
Filament Type: N600GF25 glass filled nylon
Colors Tested: Grey
Tested By: Tutley
Date Started: 07/10/19
Date Completed:

Printer Data
Bed Surface/Covering: PEI
Toolhead Types Used: v2 Titan Aero, .5 HS nozzle, w/ pt100 thermistor
Printer Type: Lulzbot mini 2
Wiper Pad Type: abs soaked polyester
Other Notes:

Manufacturer Recommended Settings
Print Temp: 290-310C
Bed Temp: N/A
Fan Speeds: N/A
Printing Speeds: 40-50mm/s
Other:

Pre-Printing Filament Assessment
Basic Use Research:

3.1 Substances

Chemical Name

CAS No.

Weight %

Exposure Limits
Polyamide 6
25038-54-4
> 70%

None
Glass fiber
65997-17-3
< 30%

None

Health or Environment Risk:

Health Hazards:

Acute toxicity -Oral: Not classified

Acute toxicity -Dermal: Not classified

Acute toxicity -Inhalation: Category 5

Skin corrosion/irritation: Not classified

Serious eye damage/eye irritation: Not classified

Respiratory sensitization: Not classified

Skin sensitization: Not classified

Germ cell mutagenicity: Not classified

Carcinogenicity: IARC 3

Reproductive toxicity: Not classified

Specific Target Organ/Systemic Toxicity (Single Exposure): Not classified

Specific Target Organ/Systemic Toxicity (Repeated Exposure): Not classified

Aspiration hazards: Not classified

Environmental Hazards:

Aquatic environmental hazards: Not classified
Chronic environmental hazards: Not classified

Disposal Options: Dispose of contents/container in accordance with regulation in a well-ventilated area.

Offer surplus and non-recyclable solutions to a licensed disposal company.
Contaminated packaging
Dispose of as unused product.

Other SDS Notes:

7.1 Precautions for safe handling
Wash thoroughly after handling. Remove contaminated clothing and wash before reuse. Use with adequate ventilation.
Minimize dust generation and accumulation. Avoid contact with eyes, skin, and clothing. Avoid ingestion and
inhalation.

7.2 Conditions for safe storage
Store in ambient temperatures. Avoid exposure to high moisture levels. No special restrictions on storage with other
products.

Appropriate engineering controls
General industrial hygiene practice.
Eye/face protection
Use equipment for eye protection tested and approved under appropriate government standards such as
NIOSH (US) or EN 166(EU).
Skin protection
Handle with gloves. Gloves must be inspected prior to use. Use proper glove removal technique (without
touching glove's outer surface) to avoid skin contact with this product. Dispose of contaminated gloves after
use in accordance with applicable laws and good laboratory practices. Wash and dry hands.
Body Protection
Choose body protection in relation to its type, to the concentration and amount of dangerous substances, and
to the specific work-place., The type of protective equipment must be selected according to the concentration
and amount of the dangerous substance at the specific workplace.
Respiratory protection
Respiratory protection is not required. Where protection from nuisance levels of dusts are desired, use type
N95 (US) or type P1 (EN 143) dust masks. Use respirators and components tested and approved under
appropriate government standards such as NIOSH (US) or CEN (EU).
Control of environmental exposure
Do not let product enter drains.

9.1 Information on basic physical and chemical properties
Appearance
: Filament, Solid
Color
: Natural and Black
Odor
: Odorless
Odor threshold
: Not available
pH
: Not applicable
Melting point/freezing point
: 215°C
Boiling point
: Not applicable
Flash point
: Not applicable
Evaporation rate
: Not applicable
Flammability
: Not available
Upper/lower flammability or explosive limits
: Not available
Vapor pressure
: Not applicable
Vapor density
: Not applicable
Relative density
: 1.2 (20 °C) Approximate

Solubility
: Soluble in alcohols
Partition coefficient (n-octanol/water)
: No data available
Auto-ignition temperature
: No data available
Decomposition temperature
: 406°C
Viscosity
: Not applicable

Packaging Notes: N/A

Minimum Bend Radius: snaps like a filled filament

Bend Test Notes: snaps clean

Bubble/Debris Test Results: no bubbles

Color Consistency: consistent color througout

Filament Diameter Variance:
2.80 (3mm from cut end)
2.83
2.84
2.85
2.83
2.83
2.83
2.84
2.83
2.84
2.81
2.81
2.82
2.84
2.84
2.82
2.84
2.84
2.82
2.80 (3mm from cut end)

Moisture Absorption:
dry wt: 7.824g
wet wt: 8.057g

Sample in AIR – DRY = 29.25 grams
Sample in AIR – WET = 29.45 grams
Air moisture absorption in 29 hrs = 0.2 grams of moisture

Sample in WATER – DRY = 26.50 grams
Sample in WATER – WET = 27.10 grams
Water moisture absorption in 29 hrs = 0.6 grams of moisture

Min Extrusion Temp: 240C

Max Extrusion Temp Before Boil: went to 385 without boiling

Min Bed Sticking Temp: ~20C (room temp)

Other Notes:

SARA 302 Components
SARA 302: No chemicals in this material are subject to the reporting requirements of SARA Title III, Section 302.

SARA 313 Components

SARA 313: This material does not contain any chemical components with known CAS numbers that exceed the
threshold (De Minimis) reporting levels established by SARA Title III, Section 313.

SARA 311/312 Hazards
No SARA Hazards

Massachusetts Right To Know Components
No components are subject to the Massachusetts Right to Know Act.

Pennsylvania Right To Know Components
Nylon 6
CAS-No.: 25038-54-4

New Jersey Right To Know Components
Nylon 6
CAS-No.: 25038-54-4

California Prop. 65 Components
This product does not contain any chemicals known to State of California to cause cancer, birth defects, or any other
reproductive harm.

Run a Control Print with an Available Comparable Material Profile
Results: needs adjustment
Profile Used: bridge nylon

Recommended Profile Changes

9��-lulzbot_hibiscus_angies-n600gf-profile-hs-001[general]
version = 2
name = angies-n600GF-profile-HS-001
definition = lulzbot_hibiscus
[metadata]
type = quality_changes
quality_type = high speed
material = Bridge_Nylon_(Taulman)_lulzbot_hibiscus
setting_version = 4
[values]
acceleration_roofing = 700
bottom_thickness = 1.4
carve_multiple_volumes = True
cool_fan_enabled = False
cool_fan_full_layer = 5
cool_min_layer_time = 10
cool_min_speed = 5
default_material_print_temperature = 250
expand_skins_expand_distance = 0
infill_pattern = lines
layer_height = 0.35
layer_height_0 = 0.4
material_bed_temperature = 40
material_bed_temperature_layer_0 = 50
material_final_print_temperature = 250
material_initial_print_temperature = 250
material_part_removal_temperature = 35
material_print_temperature = 250
material_print_temperature_layer_0 = 250
material_probe_temperature = 170
material_soften_temperature = 210
material_wipe_temperature = 190
retract_at_layer_change = True
retraction_amount = 2
retraction_combing = off
retraction_count_max = 99
retraction_hop_enabled = True
retraction_min_travel = 5
skin_preshrink = 0
skirt_gap = 5
skirt_line_count = 2
speed_layer_0 = 15
speed_print = 30
speed_slowdown_layers = 4
speed_topbottom = 30
speed_travel = 170
speed_travel_layer_0 = 70
speed_wall = 30
speed_wall_0 = 30
speed_wall_x = 30
switch_extruder_prime_speed = 10
switch_extruder_retraction_amount = 10
switch_extruder_retraction_speed = 10
switch_extruder_retraction_speeds = 10
top_bottom_thickness = 1.4
top_thickness = 1.4
PK!pBe%��2base/lulzbot_hibiscus_angies-n600gf-profile-hs-001[general]
version = 2
name = High Speed
definition = lulzbot_hibiscus
[metadata]
type = quality
quality_type = high speed
material = Bridge_Nylon_(Taulman)_lulzbot_hibiscus
setting_version = 4
[values]
backlash_fading_distance = 1.0
bottom_layers = 2
bottom_thickness = 1
brim_line_count = 10
cool_fan_full_at_height = 1
cool_fan_speed_max = 40
cool_fan_speed_min = 30
cool_min_layer_time = 10
infill_before_walls = False
layer_0_z_overlap = 0.5
layer_height = 0.38
layer_height_0 = 0.425
line_width = 0.5
material_print_temperature = 240
prime_tower_size = 7.745966692414834
raft_airgap = 0.5
retraction_amount = 1
retraction_speed = 10
skirt_brim_minimal_length = 250
speed_infill = 30
speed_layer_0 = 10
speed_print = 25
speed_topbottom = 25
speed_travel = 175
speed_wall_0 = 20
speed_wall_x = 25
support_angle = 45
support_infill_rate = 30
support_xy_distance = 1.5
top_layers = 3
top_thickness = 1
wall_thickness = 1
PK!�S
9��-lulzbot_hibiscus_angies-n600gf-profile-hs-001PK!pBe%��2base/lulzbot_hibiscus_angies-n600gf-profile-hs-001PK�

Printing Filament Assessment
Bed Adhesion Notes: seems to stick at any temp
Layer Adhesion Notes: strong!
Overhang/Bridging Notes: looks great
Color Consistency/Change: consistent color throughout
Part Removal Notes: easy to remove finished part from PEI
Other Notes:

Profile Assessment and Base Setting Recommendations
Bed Temperature Range: 22-65
Printing Temperature Range: 250C
Fan/Cooling Range: 30%-40%
Printing Speeds: 40mm/s - 50mm/s
Other Notes:

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: