Lulzbot Filament Testing Report
Manufacturer: Polymaker
Filament Type: Polamide 6 and Carbon Fibers (PA6-CF)
Colors Tested: Gray
Tested By: Angelica Suiter
Date Started: 8/13/2019
Date Completed: ---

STOP.
SDS CHECKLIST SIGN OFF: PASS
Name:_Angelica Suiter_
Date:_08/13/2019_

Printer Data
Bed Surface/Covering: Regular PEI with Gluestick
Toolhead Types Used: Workhorse Edition standard Toolhead (0.5mm nozzle)
Printer Type: Workhorse Edition
Wiper Pad Type: ABS triple coated (?)
Other Notes:

Manufacturer Recommended Settings
Print Temp: 280-300 C
Bed Temp: 25-50C (DO NOT EXCEED 50!)
Fan Speeds:OFF
Printing Speeds: 60mm/s
Other: Drying = 80 C for 12 Hrs

Pre-Printing Filament Assessment
Basic Use Research: https://us.polymaker.com/product/polymide-pa6-cf/
-https://www.tctmagazine.com/3d-printing-news/polymaker-two-fibre-reinforced-pa6-nylon-materials/
-http://www.3dtechsupplies.com.au/Products/PolyMaker/PolyMide-PA6-CF
-https://www.3dprintingsolutions.com.au/Polymaker/PolyMide-PA6-CF-Filament
-Comparable??-https://3dprintingindustry.com/news/taking-3d-printing-extreme-fiber-reinforced-pa6-250-stronger-abs-131996/

Health or Environment Risk:
“Environmental Hazards: Aquatic environmental hazards: Not classified
Chronic environmental hazards: Not classified” (sds)
“6.2 Environmental precautions
Do not flush into surface water or sanitary sewer system. Do not allow material to contaminate ground water system.6.2 Environmental precautions
Do not flush into surface water or sanitary sewer system. Do not allow material to contaminate ground water system.” (sds)
“Control of environmental exposure
Do not let product enter drains.” (sds)
Disposal Options:
“Disposal: Dispose of contents/container in accordance with regulation in a well-ventilated area.” (sds)
Other SDS Notes: --
Packaging Notes: Normal Polymaker packaging, foil bag in box.
Moisture Absorption:
Sample in AIR – DRY = 21.60 grams
Sample in AIR – WET = 21.70 grams
Air moisture absorption in 29 hrs = 0.1 grams of moisture

Sample in WATER – DRY = 22.40 grams
Sample in WATER – WET = 22.70 grams
Water moisture absorption in 29 hrs = 0.3 grams of moisture
Minimum Bend Radius: --
Bend Test Notes: --
Bubble/Debris Test Results: --
Color Consistency: --
Filament Diameter Variance: 2.88, 2.79, 2.84, 2.80,2.88, 2.84, 2.89, 2.78, 2.81, 2.81, 2.76, 2.84, 2.87, 2.86, 2.78, 2.76, 2.76, 2.77, 2.77. Average = 2.81166667
Min Extrusion Temp: --
Max Extrusion Temp Before Boil: No Boil at max temp.
Min Bed Sticking Temp: --
Other Notes: “Solubility: Soluble in alcohols” See SDS

Run a Control Print with an Available Comparable Material Profile
Results: Poor. Layers were very messy, like ramen. Too slow, too hot, etc.
Profile Used: PA6-GF High Speed

Recommended Profile Changes
--

Printing Filament Assessment
Bed Adhesion Notes: --
Layer Adhesion Notes: --
Overhang/Bridging Notes: --
Color Consistency/Change: --
Part Removal Notes: --
Other Notes: --

Profile Assessment and Base Setting Recommendations
Bed Temperature Range: --
Printing Temperature Range: --
Fan/Cooling Range: OFF
Printing Speeds: –
Other Notes: --

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: