Lulzbot Filament Testing Report
Manufacturer: Polymaker/ JF Polymers (Suzhou) Co. Ltd.
Filament Type: N600 Nylon
Colors Tested: Natural
Tested By: Samantha
Date Started: 7/10/19
Date Completed:

Printer Data
Bed Surface/Covering: PEI
Toolhead Types Used: Mini 2 standard
Printer Type: Mini 2
Wiper Pad Type: Mini 2
Other Notes:

Manufacturer Recommended Settings
Print Temp: 280-300
Bed Temp: 70-80
Fan Speeds: 0
Printing Speeds: 40-50
Other: Gluestick “if needed”

Pre-Printing Filament Assessment
Basic Use Research:
Health or Environment Risk: cat 5 inhalation
Disposal Options: well-ventilated area
Other SDS Notes: gasses may irritate eyes, nose, and throat. Wash after handling.
Packaging Notes: seems thoroughly vacuum sealed in moisture-safe bag with dessicant
Minimum Bend Radius: was able to fully fold over itself
Bend Test Notes: discolored (white) on inside and outside of bend
Bubble/Debris Test Results: no indication
Color Consistency: “freckled” with clearer looking spots. Whiter on inside of coil diameter across whole filament. Looks consistent from end-to-end
Filament Diameter Variance: 2.845 average, 2.86 max, 2.82 min, 0.04 difference
Moisture Absorption: 7.228g to 7.608g
Sample in AIR – DRY = 26.70 grams
Sample in AIR – WET = 26.80 grams
Air moisture absorption in 29 hrs = 0.1 grams moisture

Sample in WATER – DRY = 27.10 grams
Sample in WATER – WET = 28.15 grams
Water moisture absorption in 29 hrs = 1.05 grams of moisture

Min Extrusion Temp: 190
Max Extrusion Temp Before Boil: unable to determine, exceeds machine capability
Min Bed Sticking Temp: off
Other Notes: significant ooze at recommended min temp of 280

Run a Control Print with an Available Comparable Material Profile
Results: Dope AF
Profile Used: Bridge Nylon standard

Recommended Profile Changes
None

Printing Filament Assessment
Bed Adhesion Notes: Couldn’t seem to make it not stick
Layer Adhesion Notes: Seems fine with first profile test
Overhang/Bridging Notes: little bit of droop in the benchy front window (50% scale)
Color Consistency/Change: consistent semi-translucent off-white throughout print
Part Removal Notes: removed easily
Other Notes:

Profile Assessment and Base Setting Recommendations
Bed Temperature Range: 40-70
Printing Temperature Range: 230-260
Fan/Cooling Range:
Printing Speeds:
Other Notes:

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: