LulzBot Filament Testing Report

Manufacturer: Polymaker
Filament Type:	SU301C
Tested By:	D. Hall
Date:	9/22/17

Ease of use:	8/10	Filament is less brittle than previous version. (much less)

Appearance:	10/10

Color consistency:	10/10

Print temperature Range (C):	Recommended 230-240C, using 215C to start, will increase at intervals. After testing, have found that 215C to 225C works the best.

Variance in diameter: (2.81 – 2.90)

Minimum bend radius: Have been able to bend to 180 degrees, with no breaking. Tested to 360 degrees without breaking.

Prints using current Lulzbot profiles/temps:
1. “First Print” 215C with 185C standby temp
2. “ First Print” 220C with 210C standby temp
3. “First Print” 225C with 215C standby temp

Note: All prints have printed well at temperatures from 215C to 230C.
Recommend 215C to 225C.

Note: after a week of testing I have found that the filament works well (adhesion) with any PLA and Nylons. Also all Polymaker filaments. Will not adhere to ABS, HIPS, Ngen.
Most recent test, Alloy 910 print worked well. First layer had a little adhesion issue (did adhere though), may be able to clear that up with a temp change, but subsequent layers adhered well and print finished well.

General Notes:	(Be as detailed as possible)

V3 Dually used on testing
- Using glue stick. No information available. Worked well with the initial SU301 testing.
- Good adhesion, fluid layering,
- Wipe tower operates well (Cura2) no residual filament from seeping.
- Good quality on color
- Prints well at 215C , will have to test dual colors, but for support only, prints well.
- Next print at 220C, had slowed infill, (support material) better results with support material adhering.
- I have noticed that all prints work better at slower print speeds, (support material). Support material (SU301C) adheres to itself and other filament better.
- Testing Ngen now.

Recommended Print Profiles: Brent I has some profiles and I am developing more currently.

Health or environmental risks:
See SDS for information.
Nothing noted.

Disposal Options:

Recommendation:	Use standard PVA settings, with a temperature change.
Successful prints at 215 appears to get the best layering and attachment to the PLA that I am testing with. I am testing 220, currently and will increase at intervals.
All tests have been successful, with no stripping and no fails to this point.
Latest: Found that decreasing infill speed (support) and travel speed, significantly helps with print quality, specifically support material adhering to PLA.

Filament disolving:
1. Starting testing, first application: 24 oz. Water and 1 meter of filament. No agitation. Took 6 1/2 hours to dissolve. Will continue to test with denser support.

2. Test with 24 oz. Water and 1 meter of filament. Took 6 1/2 hours to dissolve. Suspect that constantly moving water will be the only thing that will make the filament dissolve more rapidly.

3. Placing print in room temperature water and leave overnight. Then you can wash out residual filament the next day. Works well.

Revision History

Revision Date	Modifications or Additions	Updated By