LulzBot Filament Testing Report

Manufacturer: Polymaker
Filament Type: SU300 Water Dissolve Filament, BVOH
Tested By: Ben Baldwin
Date:	6/28/17

Ease of use:	6/10
Appearance:	7/10
Color consistency:	8/10
Print temperature Range (C):	(200°C-220°C)
Variance in diameter: (2.85-2.95)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps:

Melting point: 150 – 230°C
Auto-ignition temperature: > 350 °C
Conditions to avoid: Temperatures above 270 °C
Dangerous Decomposition Products: carbon oxides (CO, CO2), nitrogen oxides (NO, NO2 etc.), hydrocarbons, HCN

General Notes:
- Excellent Packaging
- Resealable bag
- Spool wound slightly odd, has not affected performance, just looks strange.
- Slightly sticky feeding through guide tube

Disposal Options:

Waste Disposal Methods: Dispose of waste in accordance with applicable local, regional and international regulations and standards. Do not exceed 1mg/L in a river which the waste liquid flow into when it is disposed of from a drain as water solution.  Also, it should be diluted with water by at least 20 times when disposed of. It can be disposed of as water solution in a day with maximum 2kg as itself.

Recommendation:

Prints well with PLA, but takes some real time to dissolve in water. It is also hard and brittle after printing and can create sharp edges if pieces are removed before dissolving in water. During removal process pieces are still difficult to remove even after extensive soaking. It works best if you let it dissolve for a few days if you don’t have a large recirculating reservoir.