LulzBot Filament Testing Report

Manufacturer: Polymaker
Filament Type: SU301 Water Dissolve Filament, BVOH
Tested By: BJB
Date:	8/23/17

Ease of use:	7/10
Appearance:	7/10
Color consistency:	10/10
Print temperature Range (C):	(210°C-220°C)
Variance in diameter: (2.78-2.95)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps:

Conditions to avoid: > 270 C
Dangerous Decomposition Products: No data available

General Notes:
- Excellent Packaging
- Resealable bag
- Spool wound slightly odd, has not affected performance, just looks strange.
- No desiccant in packaging but very dry and brittle.

Disposal Options:

Waste Disposal Methods:

Recommendation: