LulzBot Filament Testing Report

Manufacturer: Polymaker
Filament Type: PolyCast
Tested By:	J. Pettit & ??
Date:	11.30.16 -

Ease of use:	X/10
Appearance:	X/10
Color consistency:	X/10
Print temperature Range (C):	(XXX-XXX/XX-XXX)
Melting point/freezing point: 135 – 210 °C
Variance in diameter: (x.xx-x.xx)
Minimum bend radius:
Prints using current Lulzbot profiles/temps:

General Notes:	(Be as detailed as possible)
- Glue stick is necessary to keep the part on the bed during printing
- Initial testing used Polylight PLA medium profile with only modifications being the print temperature at 220°C and the bed temperature at 70°C
- Onset of decomposition > 280 °C, do not print above this temperature
Early Print Pre-treatment:

Early Print Post isopropyl soak of approximately 60 minutes:

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Recommend the same profiles as used for PLA, medium quality, high quality and high speed.

Health or environmental risks:

At decomposition temperatures Carbon Oxides are released. Do not print above 280 °C

Disposal Options:

In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container. Contact manufacturer if needed.

Recommendation:

Although PLA and ABS can be used in the casting process, Polycast has advantages over both of these materials.
ABS: Prints not always good and warpage occurs for big models. It can be polished with Acetone which can be dangerous if not handled correctly. Black smoke and high residue during the casting process.
PLA: Good Printing ability, can be difficult to polish the surface to obtain a better finished model for casting. High residue during casting.
PolyCast: Good printing ability, surface polishing with isopropyl alcohol or Polysher, less residue and ash content after burning.

Revision History

Revision Date	Modifications or Additions	Updated By
11.01.16	Initial printing to determine if should be proposed to NPI for a filament to carry. Showing this portion of discovery in blue.	J. Pettit