LulzBot Filament Testing Report

Manufacturer: Polymaker
Filament Type: Trade Name Polylite PLA, Polylactic Acid Resin
Tested By: Robert
Date:

Ease of use:	10/10
Appearance:	10/10
Color consistency:	10/10
Print temperature Range (C):	(190-220/40-60)
Variance in diameter: (2.80-2.84mm)
Minimum bend radius: <25mm
Prints using current Lulzbot profiles/temps: Yes, prints well with default PLA settings

Melting point: > 140 °C
Auto-ignition temperature: > 350 °C
Conditions to avoid: Temperatures above 446F (230 °C).
Dangerous Decomposition Products: Burning produces obnoxious and toxic fumes. Aldehydes.
Carbon monoxide (CO). carbon dioxide (CO2).

General Notes:
- This comes in a brown box unlike the higher end polymaker packaging, but it still looks professional, comes on a nice spool and comes in a nice resealable bag with desiccant.
- The filament prints incredibly well and easily, and produces very consistent, high quality prints.
- No PEI treatment necessary, this sticks very well to PEI and has no troubles with warping.
- Colors are vibrant and very consistent and leaves a smooth, glossy finish. Resulting prints are very attractive.
- Amazing ease of use and consistent quality make this a great replacement as a low-cost, entry-level PLA
- This filament still comes on the nice, clear spool, but lacks the awesome remaining filament gauge that comes on other PolyMaker filaments.
- Excellent performance on overhangs and bridges

Health or environmental risks:

Mobility: No data available
Bioaccumulation: The main resin is biodegradable. Does not bioaccumulate.
Ecotoxicity effects: Data not available.

Disposal Options:

Waste Disposal Methods: In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container. Contact manufacturer if needed.

Recommendation:
I recommend that we carry this filament and promote it as the default low-cost PLA. This is a really awesome filament for the price, and is the best PLA I've used so far. The packaging, while being cheaper than that of other PolyMaker products, is still clean and professional. The filament prints easily and cleanly first time, performs remarkably well on overhangs and bridges, and sticks to the PEI consistently and with no fuss. It's cheap, prints great, and looks great every time. I will be personally buying some soon.