LulzBot Filament Testing Report

Manufacturer: Polymakr
Filament Type: PolyFlex
Tested By:	Bam, rogarbee
Date:	5.25.16

Ease of use:	9/10	*Requires flexystruder
Appearance:	8/10 (limited color options available)
Color consistency:	10/10
Print temperature Range (C):	(210-235/0-60)
Variance in diameter: (x.xx-x.xx)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps: Yes, ninjaflex, can at least double print speed

Manufacturers Properties:
Melting point: Not determined
Flash point: Not determined
Auto-ignition temperature: Not determined

General Notes:
- Same great packaging as the other new Polymaker filaments
- Well labeled reel with remaining filament markings
- No durrometer listed, but feels somewhere between Ninjaflex and Semiflex
- Prints extremely well, able to consistently extrude 10.8mm^3/s (ninjaflex tops out around 4.5mm^3/s)
- Contains 90%+ TPU with the remainder being PLA
- Currently comes in black, white, orange and yellow
- Affected by humidity, leading to blockages in the nozzle. It is shipped with a resealable bag and dessicant, which is critical for storage. After about a week in open air, it became almost unusable.

Health or environmental risks:

Dangerous Decomposition Products: Burning produces obnoxious and toxic fumes, carbon monoxide, carbon dioxide, hydrogen cyanide, nitrogen oxides, isocyanate.

Conditions to avoid: No data available

HMIS (U.S.A.):
Health Hazard: 0
Fire Hazard: 1
Reactivity: 0

Ecological:
Mobility: No data available
Bioaccumulation: Poorly biodegradable
Ecotoxicity effects: Data not available.

Disposal Options:

Waste Disposal Methods: In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container. Contact manufacturer if needed.

Recommendation: This filament requires a flexystruder, but prints extremely well. This would be a great addition to our currently small lineup of flexible materials and might make a better starter material than Ninjaflex because of it's ease of use and increased print speed.