LulzBot Filament Testing Report

Manufacturer: Polymaker
Filament Type: PolyCast
Tested By: Brent.i
Date: 6-3-19

Ease of use:	9/10
Appearance:	9/10
Color consistency:	9/10
Print temperature Range (C):	(195-230)
Variance in diameter: (2.83-2.86)
Prints using current Lulzbot profiles/temps: Yes, Polylite PLA profiles

General Notes:	(Be as detailed as possible)
- No need for gluestick
- Prints extremely well using Polylite PLA profiles
- Burns out cleaner than any other polymer the foundry as tested
- Adheres to Polydissolve

Recommended Print Profiles: High Speed, Standard, High Detail

Health or environmental risks:

Dust may irritate the eyes. Exposed may experience eye tearing, redness, and discomfort.

This product is not classified as environmentally hazardous. However, this does not exclude the possibility that large or frequent spills can have a harmful or damaging effect on the environment.

Disposal Options: Trash as a solid, burn out also applicable

Recommendation:	This product prints well, and can use existing profiles with little to no modification. With the feedback from the foundry, it is recommended to bring this on as a niche material targeted at investment casting.

Revision History

Revision Date	Modifications or Additions	Updated By