LulzBot Filament Testing Report

Manufacturer: ProtoPasta
Filament Type: Matte Fiber HTPLA
Tested By:	BAM
Date:	09.28.16

Ease of use:	7/10
Appearance:	10/10
Color consistency:	8/10
Print temperature Range (C):	(190-225/50-60)
Variance in diameter:	(2.86-2.88)
Minimum bend radius:	20mm (acceptable w/ our feed tube)
Prints using current Lulzbot profiles/temps: Yes, PP high temp PLA profiles look great

General Notes:
- The filament has the same layer/defect hiding properties as the PLA+wood filaments, resulting in a really pleasing surface texture and appearance.
  - The effect is similar to how dithering improves digital image quality.
- Prints extremely well using standard high temp PLA profiles.
- Avoid print conditions above 230°C
- Decomposition temperature: 250°C
- Prints surprisingly well at low layer heights (.14 tested on a large print w/o issues)
- Currently available in blue, white, black and red

Recommended Print Profiles: Probably just the basic 3 (fast, standard, fine); we should be good to just clone the HTPLA profiles and make minor tweaks.

Health or environmental risks:

Use in a ventilated area.

PRINCIPLE ROUTES OF EXPOSURE: Eye contact, Skin contact, Inhalation, Ingestion.
SKIN CORROSION/IRRITATION: Contact with dust/fumes may cause irritation
SERIOUS EYE DAMAGE/IRRITATION: Contact with dust/fumes may cause irritation

Disposal Options:

In accordance with local and national regulations. Do not contaminate ponds, waterways or
ditches with chemical or used container. For recycling, contact local waste disposal centers.

Recommendation:
This filament is easy to print and looks great. It is definitely approved for printing on our machines.

Revision History

Revision Date	Modifications or Additions	Updated By
9.28.16	We're actually testing this filament.	Bam