LulzBot Filament Testing Report

Manufacturer: ProtoPasta
Filament Type: PETG
Tested By: B. Baldwin
Date:	3/8/17

Ease of use:	8/10
Appearance:	9/10
Color consistency:	10/10
Print temperature Range (C):	(230-245)
Variance in diameter: (2.85-2.91)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps: Ngen
Melting Point: 100°C
Decomposition: 350°C

General Notes:
- Glue not necessary
- Do not print above 280°C.

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Ngen
Innova

Health or environmental risks:

Decomposition occurs at 350°C but it is not recommended to print above 280°C.
Decomposition products include CO and CO2

Disposal Options:

WASTE DISPOSAL METHOD: In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container. For recycling, contact local waste disposal centers.

Recommendation:	(As thorough as possible)

Proto-Patsa PET-G is an excellent co-polyester. Prints well using other PET-G like co-polyester profiles with no modification. Has an excellent finish.

Revision History

Revision Date	Modifications or Additions	Updated By