Prusa Research ABS notes:

We received 4 1 kg samples of ABS from Prusa Research; White, Yellow, Green and Blue. The blue came on a nice silver plastic spool similar to the ones we're currently getting from Alpha Plastics. The other colors came on cardboard spools that didn't spin evenly, leading to a few more snags than we're used to.

Yellow: The yellow is a nice color, and it prints much better than the yellow that we've had in stock in the past.

The diameter varied from 2.70mm to 2.91mm in a 1m sample.

Blue:

The diameter of the blue filament ranged from 2.81 to 2.91 across a 1m sample. The filament prints well using 230C and standard gcode.

Green:
the green filament printed badly on the first attempt, it appeared to be too little extrusion

The diameter of the green filament ranged from 2.82mm to 3.01mm across a 1m sample

White: The white sample looks a bit less glossy than our current white ABS, prints well at 230C and has nice consistent diameter.

The diameter in a 1m sample was very consistent, ranging from 2.84mm to 2.90mm