LulzBot Filament Testing Report

Manufacturer:	Toner Plastics
Filament Name:	Nylon 2.88mm
Filament Type:	Flexible Nylon
Date:	3/9/2015

Ease of use:	1/10
Appearance:	Semi-translucent white
Size consistency:	Great
Color consistency:	Great
Print temperature:	??? could not get it to extrude consistently
Prints using Lulzbot profiles/temps: No

Recommendation: So far I haven't been able to get this stuff to extrude consistently at any temperature. It seems to melt enough to be forced through the nozzle at around 230C, but will not extrude consistently anywhere between 230 and 270C (where the nylon is boiling).
Notes:
- Extrudes by hand @ 240C, will strip if driven at 70mm/s
- 260C print @ <10mm/s still stripper in first layer
- Extrusion quality looks great, just haven't figured out how to print it
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
2.88mm Nylon	2.84-2.89 (.05mm)	0.03mm (2.84-2.87)	???