LulzBot Filament Testing Report

Manufacturer:	Toner Plastics
Filament Name:	White PLA 3.0mm
Filament Type:	White PLA (seems like PLA/TPU blend)
Date:	2/11/2015

Ease of use:	5/10
Appearance:	Good color
Size consistency:	Good, but a bit high
Color consistency:	Good
Print temperature:	210/60 (LulzBot Mini)
Prints using Lulzbot profiles/temps: No

Recommendation: While it's a good strong, and surprisingly flexible PLA, it prints differently from general PLA, making me think that it's got some sort of elastomer additive. It does not wipe properly because of this using the standard PLA profiles, so it would have to be named/marketed as something other than basic PLA.
Notes:
- The small spool is a great size, and one of the best looking spools I've seen
- Fails bed leveling because of bad wipe
- Feels a lot like other PLA/TPU blends (polymax, saniwave PLA, etc)
- Interlayer adhesion is great, produces nice flexible parts that fail like ABS
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
3.0mm White PLA	2.94-2.97 (.03mm)	0.02mm (2.95-2.97)	190-220C (printed at 210C with standard Mini profiles)