LulzBot Filament Testing Report

Manufacturer:	Toner Plastics
Filament Name:	Yellow ABS 2.88mm, Lot # 76174
Filament Type:	Yellow ABS
Date:	1/4/2015

Ease of use:	9/10
Appearance:	Good color, but varies widely through spool
Size consistency:	Great
Color consistency:	BAD variance, from great yellow to almost natural ABS color
Print temperature:	240/110 (LulzBot Mini)
Prints using Lulzbot profiles/temps: Yes

Recommendation: This ABS prints well and forms good strong parts. The lack of color consistency is something that we would absolutely accept returns on, it makes this otherwise great ABS seem like much lower quality stuff.
Notes:
- Prints well using standard ABS settings
- We need the color issue to be addressed
- Interlayer adhesion is great, definitely strong enough to use for our in-house production.
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
2.88mm ABS / Batch # 76174	2.84-2.89 (.05mm)	0.03mm (2.86-2.89)	230-240C (printed at 240C with standard Mini profiles)