LulzBot Filament Testing Report

Manufacturer: Toner Plastics
Filament Type: PLA
Tested By:	Patrick
Date:	6/15/16

Ease of use:	9/10
Appearance:	8/10
Color consistency:	6/10
Print temperature Range (C):	(190C-230C)
Variance in diameter: (2.85-2.92)
Minimum bend radius: Under 5mm
Prints using current Lulzbot profiles/temps: Yes
Manufacturers Conditions to avoid: Temperatures above 446F (230 °C).
Manufacturers Decomposition temperature: 482F (250C)
Manufacturers Autoignition temperature: 388C

General Notes:
- Filament comes in variety of colors including translucence.
- Translucence filaments were very inconsistent.
- Inconsistent coloring seen in standard colors as well (not as prevalent)
- Reels come packaged very similar to village plastics.
- Had no problems with clogging or snapping pla.
- Some of the translucence looked really cool because they were inconsistent if they were renamed to be camo or rainbow green they would be an excellent addition to our filament lineup. The question is could the remain consistently inconsistent? (doubtful)

Health or environmental risks:

Minimal risk per MSDS

Disposal Options:

Waste from residues / unused products: In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container.

Recommendation:
Overall this filament falls short in almost every aspect to polylite pla. Some of the translucent could be added if they were renamed so that inconsistency was a feature of the filament. A couple of solid colors also showed uneven coloring. We cannot recommend carrying this filament due to inconsistency in the coloring, as we have also seen this in past samples.

Illustration 1: Shows inconsistent color