Torwell Filament testing notes:

Notes:
T-Glass
- Prints great the green looks really good.
- Sticks to the bed well.
- The diameter varies greatly I was worried about the filament stripping.
- Flex
- Has very consistent diameter for a flexible filament.
- Was the first time we printed this material through a hot end extruder and not our flexystruder.
Nylon
- Had trouble finding a good temp to print at. Started bubbling at 220 but was not sticking to itself at 210.
- It turned a green color when heated up instead of staying black.
Recommendation: .
The T-glass and Flex all printed well if we ever decide to sell 1.75 filament they would be good choices.

Filament diameter accuracy / consistency:

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
T-Glass	1.71-1.83 (.12mm)	0.04mm (1.79-1.83)	240C (printed with .4 nozzle)
Flex	1.74-1.76 (.02mm)	.01mm (1.72-1.73)	185C (printed at 190C with .4 nozzle)
Nylon	1.70-1.73 (.03mm)	.01mm (1.72-1.73)	220C (printed with .4 nozzle)
Average	1.74mm (+/- .0475mm)	0.0175mm (1.74)

Illustration 1: Flex and Nylon