LulzBot Filament Testing Report

Manufacturer: Verbatim
Filament Type: ABS
Tested By:	Baldwin
Date:	11/16/16

Ease of use:	6/10
Appearance:	5/10
Color consistency:	10/10
Print temperature Range (C):	(230-240)
Variance in diameter: (2.88-2.94)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps: Village Plastics ABS
Melting Point: 100°C
Decomposition: 300°C

General Notes:	(Be as detailed as possible)
- Glue not necessary
- Bumpy finish on filament
- Size range 2.88-2.94mm
- Packaging looks great
- Inconsistent, snaps in some places bends in others.

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Health or environmental risks:

Do not heat above decomposition temperature. carbon hydride, hydrogen cyanide, Acrylonitrile, styrene other hazardous gases can be generated.

Do not dispose of or release to the sea and water area to avoid intake by marine organism or birds.

Disposal Options:

Do not dump into sewers, on the ground or into any body of water. Burn in an adequate incinerator or bury in landfill in accordance with applicable local, state, and federal regulations.

Recommendation:	(As thorough as possible)

I had high hopes for this ABS because historically this vendor has produced quality product. Unfortunately, I found some pretty major problems with it during testing. The finish of the filament in general was wavy and varied in width quite a bit over a small distance. Also, the filament would break when bent in some places but bend in others. The print quality was average, but not anything special. Overall, I feel this product is inconsistent.

It’s hard to catch it on camera but you can see some of the inconsistencies in this picture.

Revision History

Revision Date	Modifications or Additions	Updated By