Twinclad XT coated nozzles from Micro Swiss.

Twinclad XT is a mold release coating for injection molding. It has excellent wear characteristics due to its hardness (Rc 65-67). Twinclad XT also has very low coefficient of friction(0.08). The low friction provide excellent release in molding applications, and in our case nozzle wipe sequence.

The Twinclad XT coated nozzles showed a notable increase in wear resistance and also in a machines ability to clean the nozzle before probing. Between the two machines one was prone to probe fails due to older filament. That machine failed 8 times over two days with the current non-coated nozzle, but only two times over three days with the coated nozzle. To test wear 517 grams of carbon fiber PLA was run through each nozzle. The Twinclad nozzle showed no change in the size of the orifice while the standard nozzle increased in diameter by 20 microns.

The testing shows the Twinclad is a value add for the user, however the Micro Swiss nozzle is made from 360 Brass which contains lead(≤ 3%) and also has a lower tensile strength which may lead to some breakage in the field. Overall I believe we should investigate using the coating on the AO hexagon.