Hotend Testing

Summary: Both all metal hot ends performed well at normal print speeds, however the short heat zone severely limited the printing speed compared with the budashnozzle. Also, the heatsinks on both nozzles were overkill, cooling the filament path to 50-60C just 2 fins up from the heater block at 300C. Because the performance of the nozzles is so similar and the E3D nozzle is simpler to make, it would be the better option to clone.

Change wish list:
- Change to through hole thermistor. The thermistor gets taped into a small indentation in the side of the heater block, this isn't ideal since the heater cartridge is more than enough to melt the aluminum heater block if the thermistor falls out.
- The heatsink is a bit of overkill, and the melt zone is smaller than it could be. We could get away with about half the heatsink and increase the size of the heater block without adding much to the cost or complexity.

Test Data:
	Criteria	Hexagon	E3d	Budashnozzle	AO-Hex
Performance	ABS flow (what is max flowrate of ABS (mm/s) @ 230C) (.5mm noz)	*.4noz – 165mm/s @ .175 layer / *.5 nozzle – 185mm/s @ .175mm layer	*.4mm noz – 135mm/s @ .175mm layer	*.5mm noz-275mm/s @.175mm layer / *.35mm noz – 185mm/s @ .175 layer	.5mm noz – 260mm/s @ .175mm layer
	Extrusion accuracy and consistancy	.58mm to .65mm over 1 m sample, (~45-60% over noz diameter)	Very consistant, 66-.67mm over 1 m sample (~62% over noz diameter)	.68-.71mm w/ .35noz (100% over extrusion)	.55-.56 w/.5mm noz. / Super consistent
	Slic3r config testing (do the slic3r config's we have work?)	All will need tweaking for .5mm noz	All will need tweaking for .5mm noz	Yep, they work for .35noz. Will need changes for .5mm noz.	Will need new configs
	Rated Max Temperature	400C (should probably be 300 since it's using a thermistor)	300C (400C w/ thermocouple)	235C	300C
	Nozzle temperature at 230C (thermistor)	201C	212C	188C	209C
reliability	PLA clogging (does it clog up if PLA is left in a 200C nozzle for 1 hr?))	*Not at all. (actually gave it closer to 1.5 hrs)	No clogs after 1.5 hours, just lots of oozing	No clog after 1.5 hours, however clogs have definitely been reported	No clogs after 90 min.
	Leak check (after 4 hours of printing PLA @ 190, has it started leaking?)	* On initial use, it did start leaking fairly quickly. *Tightening the nozzle completely stopped the leaking	*No apparent leaks after several hours of printing PLA	Some nozzles yes, some no. It is definitely a known issue	No leaks
	Filled filament testing to check for wear	No noticeable wear	No noticeable wear	No noticeable wear after dozens of print hours

Test descriptions
- PLA Heatsoak: I'd like to leave PLA sitting in the nozzle for an extended period of time at extrusion temperature to see if it jams the nozzle. This can sometimes be an issue with our current budashnozzle, so it'll be good to know how the Hexagon hotend reacts under the same circumstances.
  - It'll also be interesting to try this test with the heatsink fan off, just to see what happens in worst case.
- Extrusion speed testing: I'd like to see how fast we can extrude ABS @ 230C without stripping the filament. Comparing this to what we find with a regular Buda should give us a good indication of maximum print speeds, one of the main strengths of the Budashnozzle.
- Material testing: switching nozzles will probably mean we need to modify the scli3r config's for all materials. At the very least we'll need to test the configurations to see how they perform.
- High temperature material testing: the key draw of an all metal nozzle is the ability to print safely at higher temperatures than a composite nozzle such as the Buda. We need to see how this nozzle does at higher temperatures and start to come up with printing instructions and slic3r configurations for nylon, polycarbonate and other like materials.
  - We could potentially even sell a high temperature print head with one of these two nozzles for the regular TAZ.
- Leak test: The budachnozzle can leak PLA when pressurized for extended periods at extrusion temperature (ie printing). It's not a safety hazard, but it tends to dribble unsightly blobs on the print. We should run PLA at ~190C for at least a couple hours to see if this will happen with the new nozzle.
- Extrusion diameter accuracy and consistency: Filament expands when it exits the nozzle and is rapidly decompressed. It should be interesting to see how consistent and accurate the extrusion width is under similar conditions. We'll use default PLA temperatures, and extrude 1m of filament at 100mm/s, then measure the extruded filament width in several places.
- Thermal accuracy: because the temperature is read at the thermistor and not the tip of the nozzle, it's important to know how much cooler the nozzle tip is than the read temperature at the thermistor. We'll set all printers to 230 and measure with a thermocouple at the tip of the nozzle.