Unclogging procedure for Mini

If there is no filament flow at all:
1.) If they have been using PLA or PLA based materials, they shouldn't set the temperature past 250C. If they have been using other filaments they can set the temperature higher up to 290C. Turn temperature up to 250C/290C and allow nozzle to reach temperature.
2.) Open extruder idler.
3.) Pull Filament out of the extruder.
4.) Trim off end of filament.
5.) Push filament back down into the extruder and see if you can get any filament out. You can push fairly hard against the extruder to get this to work.
6.) Pull filament back out, see if there is anything stuck to the filament and trim off again.
7.) Repeat process several times to see if you can get nozzle flowing again.

If there is flow but it seems partially blocked, thin or is coming out of the nozzle all twisty:
1.) Using either HIPS or PLA turn your nozzle to the proper temperature for that material.
2.) Once up to temperature, extrude several mm of filament.
3.) Turn your temperature down, for HIPS use 140C, for PLA use 100C.
4.) Once the temperature is reached, open the extruder idler and pull out the filament.
5.) You should have a perfect mold of the inside of the hot end. The end of the filament should taper to a cylinder that is the size of your nozzle and have a nozzle sized cylinder that is about 1mm long.
6.) Check for foreign particles or gaps in your mold of the nozzle.
7.) Repeat steps as necessary to clean out nozzle.