Flexystruder 2.0 Maintenance procedure

In extended printing situations or when a flexystruder is left heated for long periods of time not printing, the Ninjaflex can degrade to a tough coating on the inside of the nozzle, causing a narrowed nozzle opening and poor extrusion. Print head function can usually be restored by cleaning out the final section of the nozzle to the full 0.6mm opening.

If a print fails or unsatisfactory parts are produced, run the following maintenance procedure to continue using the flexystruder:

- Heat the hotend to 230C, and clean the nozzle opening with an acupuncture needle or a 0.6mm drill bit
- Pinch the filament while feeding it into the flexystruder by hand, the filament shouldn't easily slip on the hobbed bolt. If it does, the toolhead will need to be reworked or replaced.
- Flush out several inches of filament by hand to make sure that there isn't still degraded filament in the nozzle
- Perform an extruder calibration and reset the eStep setting if necessary (see next page).

V2 Flexystruder Calibration Procedure

- Set the eStep value to 900 steps/mm
- Heat the extruder to 225C
- Mark the filament at 200mm from the top of the flexystruder
- Enter the following command string or run: /home/aleph/shared-j/devel/lulzbot/mini/accessories/albatross/production_docs/calibration/v2_flexy_calibration_v2.0.gcode
  - M92 E900
  - M500
  - G92 E0
  - G1 E200 F20
- Measure the amount that the flexy has under or over extruded and look up the estep value on the table below.