PEM Test Results

Torque-out

ABS
M5 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	6.1
3.7/7.4	6.1
3.8/7.6	5.8
3.9/7.8	4.4
4.0/8.0	4.4

M5 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	6.4
3.7/7.4	6.6
3.8/7.6	6.2
3.9/7.8	5.8
4.0/8.0	6.0

M3 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	2.1
2.1/4.2	2.4
2.2/4.4	2.3
2.3/4.6	2.9
2.4/4.8	2.6

M3 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	2.4
2.1/4.2	2.9
2.2/4.4	2.4
2.3/4.6	2.8
2.4/4.8	2.4

PLA
M5 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	Screw failure
3.7/7.4	Screw failure
3.8/7.6	Screw failure
3.9/7.8	Screw failure
4.0/8.0	Screw failure

M5 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	Screw failure
3.7/7.4	Screw failure
3.8/7.6	Screw failure
3.9/7.8	Screw failure
4.0/8.0	Screw failure

M3 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	2.4
2.1/4.2	2.5
2.2/4.4	2.4
2.3/4.6	2.4
2.4/4.8	2.3

M3 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	2.5
2.1/4.2	2.2
2.2/4.4	2.6
2.3/4.6	2.7
2.4/4.8	2.7

Pull-out

ABS
M5 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	3.2
3.7/7.4	3.1
3.8/7.6	3.3
3.9/7.8	2.3
4.0/8.0	2.5

M5 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	4.0
3.7/7.4	3.9
3.8/7.6	3.8
3.9/7.8	3.2
4.0/8.0	2.9

M3 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	0.8
2.1/4.2	0.9
2.2/4.4	1.2
2.3/4.6	1.0
2.4/4.8	1.0

M3 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	1.2
2.1/4.2	1.1
2.2/4.4	1.4
2.3/4.6	1.3
2.4/4.8	1.2

PLA
M5 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	3.6
3.7/7.4	3.5
3.8/7.6	3.9
3.9/7.8	3.3
4.0/8.0	3.0

M5 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
3.6/7.2	4.3
3.7/7.4	4.1
3.8/7.6	3.8
3.9/7.8	4.2
4.0/8.0	4.0

M3 - Holes in bottom
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	1.0
2.1/4.2	1.4
2.2/4.4	1.2
2.3/4.6	2.0
2.4/4.8	1.6

M3 - Holes in side
Hole Size (radius/diameter) (mm)	Torque (N.m)
2.0/4.0	1.5
2.1/4.2	1.8
2.2/4.4	1.6
2.3/4.6	1.5
2.4/4.8	1.4