LulzBot Filament Testing Report

Manufacturer:	Breathe-3DP
Filament Name:	PLA++
Filament Type:	PLA
Tested By:	Brent M
Date:	01/12/2016

Ease of use:	10/10
Appearance:	9/10
Color consistency:	10/10
Print temperature Range (C):
Melting Point (C): 180 – 220°C
Decomposition Temperature (C): 240°C
Variance in diameter: (2.82-2.85)
Minimum bend radius: NA, extremely ductile
Prints using current Lulzbot profiles/temps: Ooh yeah :) default PLA settings look great

General Notes:
- Only comes currently in 7 opaque colors, but they're nice colors
- Spool and box feel and look cheap
- Extremely ductile, feels like ABS
- Prints extremely well using default PLA settings
- Spools are labeled with an ID number
- Printed parts do much better than PLA/PHA on overhangs

Health Risks:

Eyes: No significant eye irritation or eye toxicity during normal use.
Skin: No significant skin irritation. Molten polymer may cause thermal burns.
Ingestion: May cause irritation to the throat, mouth and stomach and / or may cause nausea.
Inhalation: Inhalation of process fumes and vapors may cause irritation in the respiratory	system.
Chronic: No known chronic health effects

Environmental Risks:

Ecotoxicity: No information available.
Persistence and degradability: No information available.
Bioaccumulative potential: No information available.

Disposal Options:

Dispose of this product in accordance with local, state and federal regulations.

Recommendation: This filament is LulzBot approved, we should definitely consider this company as a PLA supplier. Size and color consistency are great, and it prints like good PLA should. They sell thins on their site for $48/kg, so it would be more of a village plastics PLA competitor than an eSun replacement.