LulzBot Filament Testing Report

Manufacturer: Innofil
Filament Type: PVA
Tested By: Ben Baldwin
Test Date(s):	7/3/17

Ease of use:	9/10
Appearance:	8/10
Color consistency:	8/10
Print temperature Range (C): 185°C
Melting Temperature: 150°C-230°C
Variance in diameter: (2.85-2.95)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps: Esun PVA
Decomposition Temperature: >300°C

General Notes:	(Be as detailed as possible)
- Do not print above 300°C
- Prints well
- very malleable ( very good thing!)
- dissolves fast

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Health or environmental risks:
Eye contact : Solid or dust may cause irritation or corneal injury due to
mechanical action.
Skin contact : It is considered to be non-irritating to skin.
Ingestion : Oral toxicity is believed to be low.
Inhalation : Single exposure to dust is not likely to be hazardous.
Fire : Under fire conditions, this polymer may decompose to form
flammable and/or explosive mixture in air.
Explosion : Dust explosion may occur, if a large amount of dust has
released in air.

Disposal Options:

Follow all relevant regulations for disposal in your country.

Recommendation:	(As thorough as possible)

This PVA is actually quite good. It runs similarly to our current offering Esun PVA. More long term storage performance testing would be needed to see how it is affected in other more moist climates. Packaging is excellent but may need to look into switching it to a resealable back for storage in in more humid climates.

Revision History

Revision Date	Modifications or Additions	Updated By
05.24.17	Creation of Innofil PVA filament testing document.	JTP