LulzBot Filament Testing Report

Manufacturer:	Biofila “Linen”
Filament Name:	Beige biodegradable filament 3.0mm
Filament Type:	biodegradable filament
Date:	3/4/2015

Ease of use:	5/10
Appearance:	Beige filament, shows layers and defects well
Size consistency:	Poor
Color consistency:	Good
Print temperature:	205/60 (LulzBot Mini)
Prints using Lulzbot profiles/temps: No, needs revised wipe

Recommendation: This stuff is a pretty cool filament and there is almost certainly a market for more earth friendly filaments. It's made from wood and algea and seems similar to PLA, although they claim superior mechanical properties.
Notes:
- Prints OK with default PLA settings
- Wipe didn't work well, but didn't fail completely. Could be made better with custom config
- Diameter consistency was poor
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
3.0mm biodegradable / filament	2.82-2.95 (.13mm)	0.05mm (2.82-2.87)	190-220C (printed at 205C with modified Mini profiles)