LulzBot Filament Testing Report

Manufacturer: ColorFabb
Filament Type: HT 5300 / Amphora
Tested By:
Date:

Ease of use:	8/10
Appearance:	8/10
Color consistency:	10/10
Print temperature Range (C):	240-260/90-110
NO temperature data available on SDS

Variance in diameter: (2.85-2.91mm)
Minimum bend radius: NA, can tie in knot
Prints using current Lulzbot profiles/temps: No, Tritan profile for mini is close

General Notes:
- Nice looking material
- Prints well at 250, 260 may give better layer adhesion
- Printed parts are more ductile than nGen but thin features can still snap
- Layer adhesion is great
- Prints stuck well to PEI at 105C and came off easily
  - For large parts that are prone to warping, glue stick can help adhesion
- Very little oozing at 250C
- At 280C and 10mm/s with low layer height prints can achieve near-perfect optical clarity, at least down through the layers. 100% concentric infill is good for this
Health or environmental risks:

Inhalation: None known.
Ingestion: None known.
Skin contact: Molten material will produce thermal burns.
Eye contact: Molten material will produce thermal burns.

This product does not contain any carcinogens or potential carcinogens as listed by OSHA, IARC or NTP.

Disposal Options:

Disposal methods: Dispose of waste and residues in accordance with local authority
requirements. Incinerate.

Recommendation:
This stuff is already printing well, and gives an alternative to ABS for higher temperature applications. The filament is definitely approved for use in Lulzbot 3D printers and would be a good candidate for a default material.