LulzBot Filament Testing Report

Manufacturer: Colorfabb
Filament Type: PETG
Tested By: Angie Suiter
Date: 1/15/18

Manufacturer Recommendations:
Nozzle temp: 235-255 C
Bed Temp: 70-80 C
Ease of use: 9/10
Appearance: 10/10
Color consistency: 10/10
Print Temperature Range (C):
Variance in diameter: +/- 0.03 mm Variance
Minimum bend radius:
Current Lulzbot profiles/temps Used for Tests:
In Test PETG Profiles for initial testing, Print Temp: 230 C
General Notes:
- Decomposition Temp: >350 C (Thermal stability not tested. Low stability hazard expected at normal printing temperatures)
- Glass Transition Temp: 70 C
- Humidity Exposure Test Print Result: PENDING CONFIRMATION TEST...
- No Packaging Notes, one test real.
- Prints well, result and reel threads are more flexible than other PETGs tested.
- Very consistent diameter readings
- no debris or inconstant texture found
- No snap point, deformation with tight bends (20mm)
- Minimum Extrusion Temp: 185 C (does extrude, does not self adhere)
- Max Extrusion Temp: 290 C (no bubbling, still not recommended)
- Oozes at 235 C
- Recommended Print Temp Range: 225 C – 250 C
- Sticks to bed with a range transition of 55 C at start – then to 50 C for bulk, because of this I do not recommend using a bed temp as high as 70 C due to the glass transition temp (BED TEMP RANGE: 50 C – 65 C)
- PETG parts for all suppliers should not be left on a heated bed for longer than a few minutes, either the part needs to be removed or the setting that keeps the bed heated needs to be turned off in the slice profile. (remove part as soon as possible for best results)
- This filament was very workable for cosmetic models but showed lower strength properties, I would like to get more colors in this mix to compare color additive effects on strength. (black, gray, white, blue, etc)
Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)
- High Speed: All profiles for toolheads recommended
- Standard: All profiles for toolheads recommended
- High Detail: All profiles for toolheads recommended
Health or environmental risks:
Do not dispose of material in bodies of water with aquatic life in it. (not in SDS)
Disposal Options:
- Material – Dispose of material waste and residues in accordance with local regulations
- Packaging – Cardboard box and/or empty filament spool can be recycled or can be disposed of in accordance with local regulations
Recommendation:
I recommend this material
Revision History

Revision Date	Modifications or Additions	Updated By
1/22/2018	Paperwork Update	A. Suiter
1/31/2018	Update	A. Suiter