LulzBot Filament Testing Report

Manufacturer: E3D Online
Filament Type: Scaffold
Tested By:	Bam
Date:	7.22.16

Ease of use:	6/10
Appearance:	8/10 (Support material, color is irrelevant)
Color consistency:	10/10
Print temperature Range (C):	(180-210/0-90)
Variance in diameter: (2.84-2.89)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps: Yes, can be used with PVA dual extrusion profiles

Manufacturers Properties:
Melting point: 150-230C
Flash point: >200C
Auto-ignition temperature: 520C

General Notes:
- Nice packaging, and interesting grey opaque color for a PVA
- Seems to be more rigid than PVA, and forms better support structures
- This PVA has been chemically modified to work better with PET materials, but also shows great adhesion to HIPS.
- Prints extremely well when package is first opened, but absorbs water very readily
- Tends to degrade quickly when the reel has absorbed water leading to clogs in nearly all prints after the first few hours of having the reel exposed to the air.
- Contains 99%+ PVA with the remainder being methanol from the manufacturing process

Health or environmental risks:

Dangerous Decomposition Products: Build-up of dangerous/toxic fumes possible in cases of
fire/high temperature.

Conditions to avoid: No data available

Ecological:
Mobility: No data available
Bioaccumulation: Readily biodegradable
Ecotoxicity effects: Data not available.

Disposal Options:

Disposal: In accordance with local and national regulations. Do not dispose of together with household
waste. Waste codes should be assigned by the user based on the application for which the product was used. Recommend putting this on product page if we carry the material since it's likely to get dumped down a drain.

Recommendation: This filament performs better than standard PVA in many ways, creating rigid, dimensionally accurate support and adhering to a wider variety of materials. That being said, if the reel is left out for even one day, it begins to clog frequently rather than just bubbling furiously. Based off of this we cannot recommend scaffold until moisture no longer causes complete failure (clogs). E3d has this filament listed as a work in progress, so we may touch base with them in the future.