Lulzbot Filament Testing Report
Manufacturer: Polymaker (JF Polymers (Suzhou) Co. Ltd. )
Filament Type: PolyMide CoPA
Colors Tested: Natural
Tested By: West
Date Started: 7/9/19
Date Completed:
CONTINUED BY: Angelica Suiter 8/16/19

Printer Data
Bed Surface/Covering: PEI
Toolhead Types Used:
Printer Type:
Wiper Pad Type:
Other Notes:

Manufacturer Recommended Settings
Print Temp: 250-265C
Bed Temp: 25-70C
Fan Speeds: 0%
Printing Speeds: 40-60mm/s
Other:
https://us.polymaker.com/Downloads/SDS/PolyMide_CoPA_SDS_V4.pdf
Glass Transition Temperature: 67˚C
Vicat Softening Temperature:180˚C
Melting Temperature: 190˚C
Drying Settings: 80˚C for 12h
Recommended Support Materials: PolyDissolve™ S1
Other:
-It is highly recommended to use the PolyBox™ when printing with PolyMide™ CoPA and to store it in the resealable bag.
-To ensure a good heat resistance of your printed part it is recommended to anneal your PolyMide™ CoPA 3d printed model.
-Annealing settings: 70˚C for 2h
-Young’s Modulus: 2223 ± 199 Mpa
-Tensile Strength: 66.2 ± 0.9 Mpa
-Bending Strength: 97.0 ± 1.1 Mpa
-Charpy Impact Strength: 9.6 ± 1.4 kJ/m2

Pre-Printing Filament Assessment
Basic Use Research:
 https://www.amazon.com/Polymaker-PolyMide-Printer-Filament-Natural/dp/B078ZR3L57/ref=sr_1_2?keywords=polymaker+copa+natural&qid=1562690686&s=gateway&sr=8-2

-“with the polybox it works perfect”

-“Amazing material - probably the strongest I've ever used, extrudes easily, and the claims of zero or near-zero warping are true. I'm printing it at 260ºC on a 70º PEI bed.”

https://www.printedsolid.com/products/polymaker-polymide-copa-nylon-1-75mm-x-750g

-“My very first print had a lot of strings in it but after a couple of prints, now it is printing so nice! It’s my favoritenfikament so far for what I’m using it for.”

Health or Environment Risk: Not likely to be an irritant in the solid form. Danger of burns when heated/molten material is handled.

Disposal Options:
In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container. Contact manufacturer if needed.
Do not flush into surface water or sanitary sewer system. Do not allow material to contaminate ground water system.

Other SDS Notes:

Avoid prolonged contact with skin and eyes. Avoid dust formation. Workers should be protected from the possibility of contact with molten material. Low hazard for usual industrial or commercial handling.

Packaging Notes: Vacuum sealed bag
Minimum Bend Radius:
Bend Test Notes:
Bubble/Debris Test: Results: No bubbles, clean of debris
Color Consistency: off white, textured gloss, consistant
Filament Diameter Variance: 2.86-2.83
Moisture Absorption:
Sample in AIR – DRY = 29.25 grams
Sample in AIR – WET = 29.35 grams
Air moisture absorption in 29 hrs = 0.1 grams of moisture

Sample in WATER – DRY = 24.45 grams
Sample in WATER – WET = 25.40 grams
Water moisture absorption in 29 hrs = 0.95 grams of moisture
Min Extrusion Temp:
Max Extrusion Temp Before Boil:
Min Bed Sticking Temp:
Other Notes:

Run a Control Print with an Available Comparable Material Profile
Results:
Profile Used:

Recommended Profile Changes

Printing Filament Assessment
Bed Adhesion Notes:
Layer Adhesion Notes:
Overhang/Bridging Notes:
Color Consistency/Change:
Part Removal Notes:
Other Notes:

Profile Assessment and Base Setting Recommendations
Bed Temperature Range:
Printing Temperature Range:
Fan/Cooling Range:
Printing Speeds:
Other Notes:

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: