Lulzbot Filament Testing Report
Manufacturer: Taulman
Filament Type: Alloy 920 Glass Fill
Colors Tested: Natural
Tested By: Angie Suiter
Date Started: 11/12/2018
Date Completed:

Printer Data
Bed Surface/Covering: Heated, PEI
Toolhead Types Used: Hardened Steel Plus
Printer Type: Mini 2
Wiper Pad Type: x2 Coated ABS
Other Notes: Rough Texture

Manufacturer Recommended Settings
Print Temp: 255 – 265 C
Bed Temp: 55 – 75 C
Fan Speeds: ---
Printing Speeds: ---
Other: ---

Pre-Printing Filament Assessment
Basic Use Research:
- https://filaments.ca/products/alloy-920-nylon-glass-fiber-1-75mm
- http://taulman3d.com/news.html
- https://taulman3d.com/index.html
- https://www.3dhubs.com/3d-printing/composites/glass-filled
https://www.reddit.com/r/3Dprinting/comments/8vn6jz/taulman_announces_glassfilled_alloy_910_carbon/
- https://www.sculpteo.com/blog/2017/04/26/welcoming-glass-filled-nylon-new-material-available-for-3d-printing/
- https://www.xometry.com/blog/glass-filled-nylon-4-things-you-need-to-know

Health or Environment Risk: “An environmental hazard cannot be excluded in the event of unprofessional handling or disposal.” Alloy 920 SDS section 12a.
Disposal Options: “Disposal should be in accordance with applicable regional, national and local laws and regulations.” Alloy 920 section 12a.
Other SDS Notes: ---
Packaging Notes: clear plastic bag, I do not think this is the finally packaging
Minimum Bend Radius: Do Not Bend
Bend Test Notes: Do Not Bend beyond reel coil, very snappy
Bubble/Debris Test Results: Consistent texture, no voids or debris
Color Consistency: Consistent, no varience
Filament Diameter Variance: 0.33 mm Variance
Average: 2.44 mm diameter average
Data points: 2.61, 2.66, 2.48, 2.56, 2.48, 2.67, 2.50, 2.69, 2.36, 2.38, 2.69, 2.62, 2.57, 2.53,	2.55, 2.56, 2.59, 2.67.
Moisture Absorption:
PHASE 1 (3ft SECTION OF FILAMENT ONLY)
Weight when opened: 0.02100 kg
Weight after Drying: 0.02195 kg
PHASE 2
Relative Humidity of Container:
Weight after 24 hours:
Min Extrusion Temp: 190
Max Extrusion Temp Before Boil: No Boil Point, extrusion fine at 290
Min Bed Sticking Temp: NO MINIMUM, sticks to PEI very well
Other Notes:

Run a Control Print with an Available Comparable Material Profile
Results: Benchy: spikes of fil on top layers that a z hop was performed on, z hop should probably be disabled; top solid layers show gapping, either needs more layers or slower top/bottom speeds; seems very strong
Profile Used: PA-CF with edits, slowed speeds, slowed retraction, lowered print temp, lower layer height.

Recommended Profile Changes

Printing Filament Assessment
Bed Adhesion Notes: sticks to PEI very well
Layer Adhesion Notes: Prints like wet sand. Increasing speed, decreasing print temp below 210, and increasing the fan can all decrease layer adhesion quality.
Overhang/Bridging Notes:
Color Consistency/Change:
Part Removal Notes:
Other Notes:

Profile Assessment and Base Setting Recommendations
Bed Temperature Range:
Printing Temperature Range:
Fan/Cooling Range:
Printing Speeds:
Other Notes:

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: