LulzBot Filament Testing Report

Manufacturer:	Verbatim
Filament Type:	TPE (PET based?)
Tested By:	bam
Date:	12/23/16

Ease of use:	7/10
Appearance:	7/10
Color consistency:	10/10
Print temperature Range (C):	(210-235/0-60)
Melting point/freezing point:	175 to 195 °C
Variance in diameter:	(2.86-2.88)
Minimum bend radius: NA
Prints using current Lulzbot profiles/temps: Prints well with ninjaflex profiles with slightly more stringing

General Notes:
- Gluestick is recommended, this material doesn’t release easily from PEI
- Do not print 300°C or above
- Has a nice almost waxy feel, not grippy like ninjaflex
  - Feels like medical device material
- Seems to string and droop a bit more than ninjaflex
- Not as high tensile strength as ninjaflex, tends to tear and permanently deform much more easily
- Currently only comes in a slightly translucent milky white

Recommended Print Profiles: For this material I think that the standard fast medium fine profiles should be fine.

Health or environmental risks:

Stable under normal storing/handling conditions. The product is stable at ambient temperature. It decomposes at temperature of 300°C and above where carbon hydride and other oxidation products (aldehyde, acid, alcohol etc.) are generated.

Disposal Options:

Do not dump into sewers, on the ground or into any body of water. Burn in an adequate incinerator or bury in landfill in accordance with applicable local, state, and federal regulations.

Recommendation:
Primalloy prints well and comes well packaged and documented like the other verbatim filaments. It prints similarly to ninjaflex but with lower tensile and yield strength, and only comes in the one color. Our recommendation is that we list the filament as LulzBot approved but that we not move forward with it until we have a more compelling reason to do so (IE customers who need a flexible that isn’t urethane based).

Revision History

Revision Date	Modifications or Additions	Updated By