A brief introduction to Begonia

Because the bed level compensation on the begonia printers depends on a very clean nozzle, the start and end g-code are super important to the print. Below I've highlighted the lines that you'll want to change if using materials other than ABS / HIPS.

It's recommended that for now you start with the most recent “stable” config which is set up for abs or HIPS (the temperature settings are in the start gcode for now).
http://devel.lulzbot.com/mini/begonia/software/2014Q3/Slic3r/z-max-home/begonia_zmax-home_ABS_0.2.ini

Printing process:
1. Spread glue-stick on the bed where the print will be. We've had good luck with spreading a new layer on top of the last for each print, then cleaning off with a razorblade or wet towel when the buildup starts affecting the prints (usually 4-5 prints).
2. Start print from gcode – all of the wiping and probing will take place at the beginning of the print.
3. Wait until bed moves forward at end of print to try to remove part. Most parts will come off easily, some water can be used to un-stick stubborn parts.

The beginning of the print:
- Printer will home to x0, y0, zMAX and begin heating both the bed and the nozzle.
- When the hot-end reaches 150C, the extruder will retract the filament out of the melt zone
- The hot-end will heat up the rest of the way to 170, giving any filament in the nozzle a chance to leak out
- The printer will then move the print-head down to the wipe pad on the back of the bed and will wipe the nozzle several times
- After wiping, the printer will use the clean nozzle to probe each of the 4 corners to find the position and tilt of the bed.
- The print head will then move to the front left corner and finish heating up
- Once the printhead is at extrusion temperature, filament will be extruded back into the nozzle and the print will begin.

Start G-code:
G92 E0
M140 S105 ; get bed heating up < - Change Sxxx to set the correct bed temperature for what you are printing
G28; home all
M109 S150 ; set to cleaning temp and wait
G1 E-25 F40 ; suck up XXmm of filament
M109 S170 ; heat up rest of way
G1 X60 Y177 F11520 ; move behind scraper
G1 Z0 ; CRITICAL: set to height of top of scraper < – Change the Zx value to fine tune how far the nozzle presses into the cleaning pad
G1 X60 Y178 F4000 ; wiping
G1 X95 Y 176 F4000 ; ""
G1 X100 Y178 F4000 ; ""
G1 X105 Y176 F4000 ; move to center
G1 X60 Y178 F4000 ; long wipe
G1 X105 Y177 F4000 ; back
G1 X60 Y177 F4000 ; forth
G1 X105 Y177 F4000 ; back
G1 X60 Y177 F4000 ; forth
G1 X110 Y177 F4000 ; back
G1 Z10 ; raise z
G28 X0 Y0 ; home x and y
G29 ; Probe
G1 X5 Y15 Z25 ; get out the way
M109 S230 ; set extruder temp and wait < – Change Sxxx to extrusion temperature for whatever you're printing
G1 Z0 E0 F1000 ; extrude filament back into nozzle
M140 S100 ; get bed temping up during first layer to cure glue < – Change Sxxx if you want a different temperature for bed after 1st later
M206 X0.0 Y0.0 Z0.0 ; offset home position for fine tuning

Troubleshooting:
If the nozzle seems too close or too far from the bed, you can change the offset in slic3r using printer settings → general → z-offset. A negative offset will bring the nozzle closer to the bed, a positive one will bring it farther away.