PEI Testing notes

- ABS: Part stuck well at 100C on the bed, parts were easily knocked off at 60C
  - large parts (4” crate) were difficult to remove when bed had cooled to 30C
  - wiping bed with wet paper towel after removing part will smooth out bed finish
  - SeeMeCNC forum recommends 80C for the bed, others 100. Will try 80C to see if 105C is just baking the part down too much
  - With moderate squish and bed at 90C an extruder body adhered well, and removing the part with bed @ 60C was similar to removing a part from PET – required prying
- PLA:
  - Adheres well and comes off of bed easily when temp drops to ~50C
  - Some corners were lifting when the bed temp was set to 65
- HIPS:
  - Adheres well, easier to knock off than ABS
- Woodfill:
- Nylon
  - Does not adhere to PEI at all
  - will stick to UHU gluestick on top of PEI surface
  - UHU glue might also be used to smooth out and scratches in the PEI
- PVA
- Bronzefill

What the internets are saying about it:
- Yes with ABS. I don't think PEI is suitable for nylon, at least no one I've heard has tried it.

  There are a few tricks; 1) use the lowest bed temperature that gets good stick 2) remove the part immediately, don't allow the bed to cool 3) if during 2 the part is difficult to remove or if y9ou wait until the bed has cold, chill the bed/part in the refrigerator and it will literally SNAP off!
- Not to room temp, but if you keep cooling to fridge temps, then yes.
- You still need to use borosilicate if you plan to heat, especially at ABS temps.

  It is pretty easy to remove, I've done it twice!
- Make sure to clean the PEI with rubbing alcohol (or acetone) well then try it. A little trick I use - BUT PLEASE READ THIS CAREFULLY - is to use 2000 grit (do NOT USE anything courser than this) and gently sand the surface. I get 100% stick for dozens of prints then do this again. Been working this way for months now with "0" failures.
- I use it dry. Works fine that way. DON'T use a lot of pressure, you are just trying to scuff the surface a little. Then I wipe with a bit of alcohol and I'm good to go for dozens of prints.
- Ah, I looked back, you are printing with ABS! Yes, much higher temp on the bed. I print at 80°C for ABS and 55° for PLA on PEI. Try raising the temperature, it really makes a big difference with PEI.
- I use 90c with PEI and ABS, sticks well.