FAILURE ANALYSIS REPORT

NAME: Brent MacKenzie	DATE: 11/24/2014
ITEM DESCRIPTION: / Hexagon hotend nozzle –Lulzbot edition	SERIAL NO: / Multiple
FAILURE REPORT DATE: 11/24/2014	ORIGIN: Internal

FAILURE MODE/ DESCRIPTION: / The nozzle starts leaking below the heater block in the first few hours of printing. Trying to tighten the nozzle reveals that the nozzle is sheared off at the base of the threads. This has been seen 3 times since the production of the first 13 Lulzbot Mini machines, and had not been seen previously in the ~40 machines from the Begonia and Camillia phases over a combined several hundred hours of testing.	SYMPTOMS: / Filament leaking out from between the nozzle and the heater block / When trying to tighten the nozzle, it easily falls out of the heater block, broken at the base of the threads / The failure occurred in the thin lower section of the nozzle, where no contact is made with the threads and the nozzle is presumably under tension from tightening

OBSERVATIONS & FINDINGS & PICTURES / The observed failed nozzles broke in a similar pattern and location as several that were deliberately overtightened to induce failure / The nozzles did not appear to break until sometime immediately after they were tightened in final calibration then heated up to 230 to print a calibration octopus. Failure was observed in < 2 print hours after this step in all 3 cases. / 85 nozzles were disassembled as received from RRD before any of our assembly processes. They were assembled to a fairly consistent tightness, but all seemed quite a bit tighter than they are when we assemble them in house. / Of the 40 nozzles that were inspected under a microscope, one has what appeared to be double cut threads (2 distinct troughs and noticeably thinner threads). The 2 broken nozzles that were recovered didn't show this defect, so it's most likely not the root cause. / Above: Photos of one of the 3 failed nozzles in the field / Below: Photos of a new nozzle intentionally overtightened to failure / Below: Comparison of the 2 field failures observed / Below: Double cut threads on the upper extension, normal below. Not the cause of this failure but good to know about. Found 1 like this in a sample size of 40 hotends, looks like the die cut extra material away while backing off.

CONCLUSION/ ROOT CAUSE: / I believe that the failures are the result of overly tightened nozzles breaking as they heat up and the thread run-out section of the nozzle is stretched further. Based on the CTE of Brass and Aluminum, heating a tight nozzle from room temp to 280C could induce a tensile stress of up to 100 Mpa, about 40% of the yield strength of brass and ~15% of the ultimate strength. It's not enough to cause a nozzle to fail on it's own but it's certainly enough to push it over the edge if it's already close. / 2 of the changes that were applied in this batch of hotends were that the nozzles came to us already VERY tightly screwed into the heater block, and that we added a final tightening of the nozzle using channel locks and a 7mm wrench when the hotend had reached 170C. / Between the nozzles being tighter than expected when received, our extra tightening and the high temperatures of the hotend it's likely that the nozzles are failing on heat up due to thermal expansion in addition to the over tightened threads.

CORRECTIVE ACTIONS/ FIXES	OWNER	COMPLETION DATE
Re-write assembly documentation to loosen the nozzle and reset at a lower tension. Also, nix the final tightening of the nozzle at temperature. Rework 45 toolheads with new process and mount to all available Camillia and Croaton printers to test	Brent M	11/25/2014
Request that all future shipments come unassembled, and find torque wrench for accurately setting nozzle tension for production runs	Brent M	11/26/2014